ISOFIN-P INDUSTRY & TECHNOLOGY

# ISOFIN-P Product Catalog

Waterproofing · Insulation · Protection · D&G HOLDING, 1 rue de Stockholm, 75008 Paris

ISOFIN-P offers professional solutions for waterproofing, thermal and acoustic insulation, fire protection and building renovation. Our products are CE-certified per EN 1504-2:2004, covering 34 tested and certified products.

## 1 · ISOFIN-P SB SUPER COMPONENT

Extremely durable coating composed of polymer components, with strong adhesion, excellent water and UV resistance. Does not wear thanks to its elastic structure. Ideal for concrete surfaces and terraces.

| Property | Value |
| --- | --- |
| Density (g/mL) | 1.40 ± 0.10 |
| pH | 7.0 – 9.0 |
| Water transmission (kg/m².h) | 10500–14500 |
| Adhesion (N/mm²) | 74 ± 2 |
| Vapour permeability | 5 ≤ SD ≤ 50 Class II |
| Solvent | Water |
| Fire class | B S1 d0 |
| Color | All colors available |
| Packaging | 5, 10, 18 kg PP buckets |

## 2 · ISOFIN-P MS POLIA

Pure polymer with excellent properties. Ready to use, UV resistant, glossy, elastic structure. Exterior insulation for terraces, roofs, facades, concrete, plaster, wood, metal.

| Property | Value |
| --- | --- |
| Density (g/mL) | 1.30 ± 0.10 |
| pH | 7.0 – 9.0 |
| Viscosity (mPa.s) | 16000–18000 |
| Solid content (%) | 70 ± 2 |
| Water transmission | < 0.1 Class W3 |
| Vapour permeability | 5 ≤ SD ≤ 50 Class II |
| Solvent | Water |
| Fire class | B S1 d0 |
| Packaging | 5, 10, 18 kg |

## 3 · ISOFIN-P MS POLYMER

Pure polymer 300% elastic. Ready to use, UV resistant, glossy. Exterior insulation for terraces, roofs, wet areas, concrete, wood, metal.

| Property | Value |
| --- | --- |
| Density (g/mL) | 1.05 ± 0.10 |
| pH | 7.0 – 9.0 |
| Viscosity (mPa.s) | 13000–15000 |
| Solid content (%) | 46 ± 2 |
| Water transmission | < 0.1 Class W3 |
| Vapour permeability | 5 ≤ SD ≤ 50 Class II |
| Solvent | Water |
| Fire class | D-s2 d0 |
| Packaging | 5, 10, 18 kg |

## 4 · ISOFIN-P M 36

Ready-to-use mortar that blocks water in 40 seconds. For water leaks and surface water. Does not shrink.

| Property | Value |
| --- | --- |
| Setting time (sec) | 40–50 |
| Solvent | Water |
| Color | Grey |
| Fire class | A2 S1 d0 |
| Packaging | 5, 10, 18 kg |

## 5 · ISOFIN-P A4

Crack filling mastic. Ready to use for cracks and joints in concrete and plaster.

| Property | Value |
| --- | --- |
| Density (g/mL) | 1.40 ± 0.10 |
| pH | 7.0 – 9.0 |
| Vapour permeability | SD < 5m Class I |
| Solvent | Water |
| Fire class | B S1 d0 |

## 6 · ISOFIN-P MS 80

Transparent product giving a natural look to absorbent surfaces. Does not form a layer. Prevents dirt and erosion.

| Property | Value |
| --- | --- |
| Density (g/mL) | 0.75 ± 0.10 |
| pH | 7.0 – 9.0 |
| Solvent | Water |
| Color | Transparent |
| Fire class | B fl S1 |

## 7 · ISOFIN-P MS 82

Anti-condensation paint for basements, garages, moisture-exposed walls. Prevents mold and condensation.

| Property | Value |
| --- | --- |
| Density (g/mL) | 1.50 ± 0.10 |
| Viscosity (mPa.s) | 2000–4000 |
| Vapour permeability | 5 ≤ SD ≤ 50 Class II |
| Color | Off-white |
| Fire class | B fl S1 |

## 8 · ISOFIN-P BD

Transparent floor insulation. Does not form a layer. Transparent, UV resistant. Absorbent surfaces: plaster, concrete, aerated concrete.

| Property | Value |
| --- | --- |
| Density (g/mL) | 0.90 ± 0.10 |
| pH | 7.0 – 9.0 |
| Color | Transparent |
| Solvent | Water |

## 9 · ISOFIN-P M 03

Elastic waterproof repair mortar. High adhesion. Repair of cracks, holes, concrete defects.

| Property | Value |
| --- | --- |
| Solvent | Water |
| Fire class | A2 S1 d0 |
| Packaging | 20 kg bag |

## 10 · ISOFIN-P D10 LATEX

Liquid improving mortar properties. Enhances adhesion and elasticity. Prevents cold joints.

| Property | Value |
| --- | --- |
| Density (g/mL) | 0.90 ± 0.10 |
| pH | 7.0 – 9.0 |
| Viscosity (mPa.s) | 500–1500 |
| Solid content (%) | 18 ± 2 |
| Vapour permeability | 5 ≤ SD ≤ 50 Class II |
| Solvent | Water |

## 11 · ISOFIN-P SHINE FLOOR

Two-component polyurethane floor coating. Glossy or matte. UV, wear, impact resistant. Excellent adhesion.

| Property | Value |
| --- | --- |
| Density (g/mL) | 1.20 ± 0.10 |
| Vapour permeability | SD ≤ 5 Class I |
| Viscosity (mPa.s) | 1000–4000 |
| Solvent | Solvent-based |
| Fire class | B fl S1 |

## 12 · ISOFIN-P LIQUID MARBLE

Decorative solvent-free floor coating. 3D marble effect. Resistant, easy to clean. Interior only.

| Property | Value |
| --- | --- |
| Density (g/mL) | 1.10 ± 0.10 |
| Vapour permeability | 5 ≤ SD ≤ 50 Class II |
| Viscosity (mPa.s) | 1500–3500 |
| Solvent | Solvent-free |
| Fire class | C fl S1 |

## 13 · ISOFIN-P ANTI FIRE PAINT

Fire-retardant finishing paint. Intumescent on contact with fire, forms an insulating layer. Water-based, solvent-free.

| Property | Value |
| --- | --- |
| Density (g/mL) | 1.40 ± 0.10 |
| pH | 7.0 – 9.0 |
| Viscosity (mPa.s) | 12500–15000 |
| Vapour permeability | 5 ≤ SD ≤ 50 Class II |
| Solvent | Water |
| Fire class | B S1 d0 |

## 14 · ISOFIN-P THERMAL PAINT

Thermal insulation paint. Reduces heat in summer, retains coolness. Reduces energy bill. Prevents mold and condensation.

| Property | Value |
| --- | --- |
| Density (g/mL) | 0.70 ± 0.15 |
| pH | 7.0 – 9.0 |
| Viscosity (mPa.s) | 12500–13500 |
| Solid content (%) | 48 ± 2 |
| Vapour permeability | 5 ≤ SD ≤ 50 Class II |
| Thermal cond. (W/mK) | 0.060–0.080 |
| Solvent | Water |
| Fire class | B S1 d0 |

## 15 · ISOFIN-P STREET PAINT

One-component UV and water resistant floor paint. All colors. For asphalt, concrete, sports grounds.

| Property | Value |
| --- | --- |
| Density (g/mL) | 1.40 ± 0.10 |
| pH | 7.0 – 9.0 |
| Viscosity (mPa.s) | 9000–12000 |
| Vapour permeability | 5 ≤ SD ≤ 50 Class II |
| Solvent | Water |
| Fire class | B S1 d0 |

## 16 · ISOFIN-P LIQUID GLASS

Transparent high-resistance waterproofing. UV and weather resistant. For decorative surfaces, ceramics, glazing.

| Property | Value |
| --- | --- |
| Color | Transparent |
| Solvent | Water |
| UV resistant | Yes |

## 17 · ISOFIN-P SS SOIL HARDENER

Concentrate to harden and stabilize soil. Transparent after drying. Compliant PM10 and PM2.5. For roads and platforms.

| Property | Value |
| --- | --- |
| pH | 7.0 – 10.0 |
| Viscosity (mPa.s) | 4000–9000 |
| Solvent | Water |
| Fire class | B S1 d0 |

## 18 · ISOFIN-P UNIVERSAL PRIMER

Deep-penetrating primer. Prepares surface for insulation and paint. Excellent adhesion. Quick drying.

| Property | Value |
| --- | --- |
| Density (g/mL) | 1.00 ± 0.10 |
| pH | 7.0 – 9.0 |
| Viscosity (mPa.s) | 8000–10000 |
| Vapour permeability | 5 ≤ SD ≤ 50 Class II |
| Solvent | Water |
| Fire class | B S1 d0 |

## 19 · ISOFIN-P EP PRIMER

Transparent solvent-free epoxy primer. Two-component. Excellent adhesion. Fills concrete voids.

| Property | Value |
| --- | --- |
| Vapour permeability | SD ≤ 5 Class I |
| Solvent | Solvent-free |

## 20 · ISOFIN-P ANTI RUST PRIMER

Anti-corrosion primer for metal surfaces. Protects iron and steel from rust.

| Property | Value |
| --- | --- |
| Color | Red / Blue |
| Solvent | Solvent-based |

## 21 · ISOFIN-P MD 28

700% elastic coating for waterproofing. High resistance. Strong adhesion on dry or damp surfaces.

| Property | Value |
| --- | --- |
| Density (g/mL) | 1.00 ± 0.10 |
| pH | 7.0 – 9.0 |
| Viscosity (mPa.s) | 8000–10000 |
| Vapour permeability | 5 ≤ SD ≤ 50 Class II |
| Solvent | Water |
| Fire class | B S1 d0 |

# Certifications

- CE Certificate — EN 1504-2:2004 — No. 2765-CPR-0136

- ISO 9001 — Quality Management

- SZUTEST — Notified Body

- TSE — Turkish Standard

- 34 CE-certified products

- Valid until 07.08.2027

# Contact Information

| Company | D&G HOLDING |
| --- | --- |
| Address | 1 rue de Stockholm, 75008 Paris, France |
| Phone | +33 6 51 81 82 29 |
| Email | contact@isofinp.com |
| Website | www.isofinp.com |
| Brand | ISOFIN-P |

ISOFIN-P INDUSTRY & TECHNOLOGY · D&G HOLDING · 1 rue de Stockholm, 75008 Paris · contact@isofinp.com · www.isofinp.com