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ISOFIN-P offers professional solutions for waterproofing, thermal and acoustic insulation, fire protection and building renovation. Our products are CE-certified per EN 1504-2:2004, covering 34 tested and certified products.
1 · ISOFIN-P SB SUPER COMPONENT
Extremely durable coating composed of polymer components, with strong adhesion, excellent water and UV resistance. Does not wear thanks to its elastic structure. Ideal for concrete surfaces and terraces.
	Property
	Value

	Density (g/mL)
	1.40 ± 0.10

	pH
	7.0 – 9.0

	Water transmission (kg/m².h)
	10500–14500

	Adhesion (N/mm²)
	74 ± 2

	Vapour permeability
	5 ≤ SD ≤ 50 Class II

	Solvent
	Water

	Fire class
	B S1 d0

	Color
	All colors available

	Packaging
	5, 10, 18 kg PP buckets


2 · ISOFIN-P MS POLIA
Pure polymer with excellent properties. Ready to use, UV resistant, glossy, elastic structure. Exterior insulation for terraces, roofs, facades, concrete, plaster, wood, metal.
	Property
	Value

	Density (g/mL)
	1.30 ± 0.10

	pH
	7.0 – 9.0

	Viscosity (mPa.s)
	16000–18000

	Solid content (%)
	70 ± 2

	Water transmission
	< 0.1 Class W3

	Vapour permeability
	5 ≤ SD ≤ 50 Class II

	Solvent
	Water

	Fire class
	B S1 d0

	Packaging
	5, 10, 18 kg


3 · ISOFIN-P MS POLYMER
Pure polymer 300% elastic. Ready to use, UV resistant, glossy. Exterior insulation for terraces, roofs, wet areas, concrete, wood, metal.
	Property
	Value

	Density (g/mL)
	1.05 ± 0.10

	pH
	7.0 – 9.0

	Viscosity (mPa.s)
	13000–15000

	Solid content (%)
	46 ± 2

	Water transmission
	< 0.1 Class W3

	Vapour permeability
	5 ≤ SD ≤ 50 Class II

	Solvent
	Water

	Fire class
	D-s2 d0

	Packaging
	5, 10, 18 kg


4 · ISOFIN-P M 36
Ready-to-use mortar that blocks water in 40 seconds. For water leaks and surface water. Does not shrink.
	Property
	Value

	Setting time (sec)
	40–50

	Solvent
	Water

	Color
	Grey

	Fire class
	A2 S1 d0

	Packaging
	5, 10, 18 kg


5 · ISOFIN-P A4
Crack filling mastic. Ready to use for cracks and joints in concrete and plaster.
	Property
	Value

	Density (g/mL)
	1.40 ± 0.10

	pH
	7.0 – 9.0

	Vapour permeability
	SD < 5m Class I

	Solvent
	Water

	Fire class
	B S1 d0


6 · ISOFIN-P MS 80
Transparent product giving a natural look to absorbent surfaces. Does not form a layer. Prevents dirt and erosion.
	Property
	Value

	Density (g/mL)
	0.75 ± 0.10

	pH
	7.0 – 9.0

	Solvent
	Water

	Color
	Transparent

	Fire class
	B fl S1


7 · ISOFIN-P MS 82
Anti-condensation paint for basements, garages, moisture-exposed walls. Prevents mold and condensation.
	Property
	Value

	Density (g/mL)
	1.50 ± 0.10

	Viscosity (mPa.s)
	2000–4000

	Vapour permeability
	5 ≤ SD ≤ 50 Class II

	Color
	Off-white

	Fire class
	B fl S1


8 · ISOFIN-P BD
Transparent floor insulation. Does not form a layer. Transparent, UV resistant. Absorbent surfaces: plaster, concrete, aerated concrete.
	Property
	Value

	Density (g/mL)
	0.90 ± 0.10

	pH
	7.0 – 9.0

	Color
	Transparent

	Solvent
	Water


9 · ISOFIN-P M 03
Elastic waterproof repair mortar. High adhesion. Repair of cracks, holes, concrete defects.
	Property
	Value

	Solvent
	Water

	Fire class
	A2 S1 d0

	Packaging
	20 kg bag


10 · ISOFIN-P D10 LATEX
Liquid improving mortar properties. Enhances adhesion and elasticity. Prevents cold joints.
	Property
	Value

	Density (g/mL)
	0.90 ± 0.10

	pH
	7.0 – 9.0

	Viscosity (mPa.s)
	500–1500

	Solid content (%)
	18 ± 2

	Vapour permeability
	5 ≤ SD ≤ 50 Class II

	Solvent
	Water


11 · ISOFIN-P SHINE FLOOR
Two-component polyurethane floor coating. Glossy or matte. UV, wear, impact resistant. Excellent adhesion.
	Property
	Value

	Density (g/mL)
	1.20 ± 0.10

	Vapour permeability
	SD ≤ 5 Class I

	Viscosity (mPa.s)
	1000–4000

	Solvent
	Solvent-based

	Fire class
	B fl S1


12 · ISOFIN-P LIQUID MARBLE
Decorative solvent-free floor coating. 3D marble effect. Resistant, easy to clean. Interior only.
	Property
	Value

	Density (g/mL)
	1.10 ± 0.10

	Vapour permeability
	5 ≤ SD ≤ 50 Class II

	Viscosity (mPa.s)
	1500–3500

	Solvent
	Solvent-free

	Fire class
	C fl S1


13 · ISOFIN-P ANTI FIRE PAINT
Fire-retardant finishing paint. Intumescent on contact with fire, forms an insulating layer. Water-based, solvent-free.
	Property
	Value

	Density (g/mL)
	1.40 ± 0.10

	pH
	7.0 – 9.0

	Viscosity (mPa.s)
	12500–15000

	Vapour permeability
	5 ≤ SD ≤ 50 Class II

	Solvent
	Water

	Fire class
	B S1 d0


14 · ISOFIN-P THERMAL PAINT
Thermal insulation paint. Reduces heat in summer, retains coolness. Reduces energy bill. Prevents mold and condensation.
	Property
	Value

	Density (g/mL)
	0.70 ± 0.15

	pH
	7.0 – 9.0

	Viscosity (mPa.s)
	12500–13500

	Solid content (%)
	48 ± 2

	Vapour permeability
	5 ≤ SD ≤ 50 Class II

	Thermal cond. (W/mK)
	0.060–0.080

	Solvent
	Water

	Fire class
	B S1 d0


15 · ISOFIN-P STREET PAINT
One-component UV and water resistant floor paint. All colors. For asphalt, concrete, sports grounds.
	Property
	Value

	Density (g/mL)
	1.40 ± 0.10

	pH
	7.0 – 9.0

	Viscosity (mPa.s)
	9000–12000

	Vapour permeability
	5 ≤ SD ≤ 50 Class II

	Solvent
	Water

	Fire class
	B S1 d0


16 · ISOFIN-P LIQUID GLASS
Transparent high-resistance waterproofing. UV and weather resistant. For decorative surfaces, ceramics, glazing.
	Property
	Value

	Color
	Transparent

	Solvent
	Water

	UV resistant
	Yes


17 · ISOFIN-P SS SOIL HARDENER
Concentrate to harden and stabilize soil. Transparent after drying. Compliant PM10 and PM2.5. For roads and platforms.
	Property
	Value

	pH
	7.0 – 10.0

	Viscosity (mPa.s)
	4000–9000

	Solvent
	Water

	Fire class
	B S1 d0


18 · ISOFIN-P UNIVERSAL PRIMER
Deep-penetrating primer. Prepares surface for insulation and paint. Excellent adhesion. Quick drying.
	Property
	Value

	Density (g/mL)
	1.00 ± 0.10

	pH
	7.0 – 9.0

	Viscosity (mPa.s)
	8000–10000

	Vapour permeability
	5 ≤ SD ≤ 50 Class II

	Solvent
	Water

	Fire class
	B S1 d0


19 · ISOFIN-P EP PRIMER
Transparent solvent-free epoxy primer. Two-component. Excellent adhesion. Fills concrete voids.
	Property
	Value

	Vapour permeability
	SD ≤ 5 Class I

	Solvent
	Solvent-free


20 · ISOFIN-P ANTI RUST PRIMER
Anti-corrosion primer for metal surfaces. Protects iron and steel from rust.
	Property
	Value

	Color
	Red / Blue

	Solvent
	Solvent-based


21 · ISOFIN-P MD 28
700% elastic coating for waterproofing. High resistance. Strong adhesion on dry or damp surfaces.
	Property
	Value

	Density (g/mL)
	1.00 ± 0.10

	pH
	7.0 – 9.0

	Viscosity (mPa.s)
	8000–10000

	Vapour permeability
	5 ≤ SD ≤ 50 Class II

	Solvent
	Water

	Fire class
	B S1 d0


Certifications
1. CE Certificate — EN 1504-2:2004 — No. 2765-CPR-0136
1. ISO 9001 — Quality Management
1. SZUTEST — Notified Body
1. TSE — Turkish Standard
1. 34 CE-certified products
1. Valid until 07.08.2027
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